5666 Central Ave.

Indianapolis In. 46220				                                                                           (317)710-2136

## Fax (317)251-3474

## Email: softheatmfg@gmail.com

Soft Heat Melter and Reclaimer Operating Instructions

WARNING: Follow all safety precautions and all directions per these instructions.  Failure to follow instructions and to exercise responsible care may result in damage, injury, or death.  When charging Kettle with material, you must wear goggles, gloves, and long sleeved clothing.

- Position the kettle so that it will be at least six (6) feet from combustible material. Charge kettle or reclaimer with the proper amount of crack filler or reclaimable asphalt respectively. (50 pounds for 10 gal. unit) (Removed from the cardboard box) Plastic bag will melt into heated crack filler when stirred. Asphalt pieces are placed on inner grating and drop through grating when hot. Material is accessed through shovel door.

- Light the LP burner as described noting to ALWAYS allow any unburnt propane to clear box before lighting. On all units with spark ignition, bring pressure up at regulator slowly while depressing ignitor button. A faint sound of ignition can be heard and heat will be felt at vents. Release ignitor button. Allow burner to warm and slowly bring regulator pressure to full setting.

- Main burner of AR55 reclaimer is located on the underside of the lid. Fully open lid and make sure no Twin Pack guards are installed. With regulator set at 18 PSI, turn brass valve on top of lid to begin hearing propane escape while passing a hand held torch over the burner surface. Heat will be felt upon ignition but is hard to see in sunlight. ( it is recommended to practice this lighting procedure in low light to help familiarize users to the characteristics of a properly lit AR55 top burner) At low valve settings, a wandering blue flame will be present. Allow the mat to warm gradually by slowly increasing gas flow until an orange color is present across the entire mat at the fully open valve setting.** Caution** this burner is now operating at 927 degrees fehrenheit. Close lid over loaded grating until all material has fallen below into holding chamber. To reload grating shut off burner and open lid. Be mindful not to touch any hot surface. Repeat lighting and closure process.

- The lower burner of an AR55 reclaimer is a traditional torch. After lighting torch, insert into the kettle burner well without smothering the flame. **Note: If the torch is inserted into the burner well when the flame is running full, it is likely to be smothered before it can start an updraft.  If the torch is smothered while in the burner well of the kettle, it is extremely important to allow any unburned gas in the burner well to vent before reinserting the torch.  If wind is a factor, locate the AR55 kettle so the burner is operating down wind.  Shielding may also be necessary.

- Make certain the torch is positioned properly in the center of the burner well and adjust flame at valve on torch.  Remove any obstructions.

- On all units, after waiting a moment to allow the circulation of air to start around the pan, the regulating valve can be adjusted as needed. Do not exceed 18 PSI at any gauged regulator. Non gauged regulators are set to not exceed maximum propane delivery and should never be turned tightly.

- Any of the crack sealant kettles are designed to draw off liquid for use as soon as pouring temperature is reached.  While heating, remember that heat penetrates the block of sealant material slowly.  Waiting for the blocks to completely melt is inefficient and time consuming.  For best results and fastest melting rate, crack sealant material should be used as it liquefies.  When operating at high flame, stir the material frequently.  Extended heating of sealant material over 400 degrees F. will destroy the elastomeric polymers.

- Stir material prior to drawing off.  Stirring will increase melting rate and keep any unmelted portion of polybag away from draw off valve.

- Flashing can be completely prevented by not allowing the material to exceed 400 degrees F.  If the material does become too hot, turn the propane off immediately.  For regular operation of lower burner on AR55, no more than half the normal flame on the torch gives sufficient heat to maintain reclaimed material temperature or plant supplied material when used as a” hot box” with grating removed.  If flashing does occur, close the cover immediately.  NEVER use water to extinguish a kettle fire, and always have an extinguisher available rated to combat oil fires.

- It is not essential to drain a sealant Kettle at the end of the day.  However, the least amount of material left in the Kettle, the easier start up will be with the next use. AR55 reclaimers should be shoveled clean and unused material simply formed in uniform sizes to cool and be reclaimed another day.  WARNING: NEVER allow any burner to fire into an empty Kettle!

10. Do not cover any kettle vent holes while the burner is in operation, or you will stop               the draft and smother the flame.  To prevent water from collecting in the pan, cover the kettle whenever it is stored.

Soft Heat Mfg. LLC warrants only that this product conforms, at the time of delivery from manufacturing facility, to Soft Heat Mfg. LLC specifications.  All other warranties, expressed or implied are excluded.  All claims for breach of warranty or defective product must be made within one month of the date of purchase.

Inspected & Checked by:______________________________  Date:___________